OXY/ACETYLENE SET UP & SHUT DOWN PROCEDURE

**Before attaching regulators to a new tank, crack cylinder valves to blow out dust,

moisture, etc.**

**When opening tank valves, ALWAYS open valves slowly so pressure on regulators is

NOT sudden!!!!

LIGHTING SEQUENCE

1.  	Make sure regulator T-handles are turned out loose.

2.  	Open acetylene torch valve 1/2 turn.

4. 	Screw in acetylene regulator T-handle adjusting valve to working pressure (For

welding, always use tip size for pressure).

- Turn off acetylene torch valve (you will have purged the acetylene line at the same

time).

7.  	Open oxygen torch valve 1/2 turn.

- Screw in the oxygen T-handle adjusting valve to working pressure (For welding,

always use tip size for pressure).

9.  	Turn off oxygen torch valve (you will have purged the oxygen line).

- Open acetylene torch valve 1/4 turn, light acetylene. (use friction-type lighter only).

(NEVER LIGHT THE OXY/ACETYLENE TORCH WITH A MIXED GAS!!!!!!!)

Adjust flame until 29 c.f. of acetylene flowing (flame turns blue or turns transparent about 3/4” from the end of the tip).

- For welding the mild steel, Open oxygen torch valve and adjust to neutral flame.

- For Brazing or Bronze welding mild steel, Open oxygen torch valve and adjust to a slightly oxidizing flame.

SHUT DOWN SEQUENCE

1.  	Close acetylene torch valve first, then close oxygen torch valve.

- Back out the Acetylene regulator T-handle until loose---Open acetylene torch valve to release the pressure off regulator---Close torch valve.

- Back out the Oxygen regulator T-handle until loose---Open oxygen torch valve to release the pressure off regulator---Close torch valve

5.  	Take tip out of torch body and replace in storage hanger.

- Hang up spark lighter and pliers

- Replace any filler metal back to storage shelf.

- Coil hose up and hang on hanger.

9.	Turn stool upside down and place on welding station.